F10 Clause 355 Masterblock – Masterlite Pro Acoustic

Aggregate Industries UK Ltd, North End, Ashton Keynes, Wiltshire - Tel: 01285 646900 - Fax: 01285 646949

- Website: wwww.aggregate.com/concrete-blocks

Please press CTRL and click on a product below to go to the Specification (all below)

Masterlite Pro Acoustic 100mm

Masterlite Pro Acoustic 140mm

F10 Clause 355 – Masterlite Pro Acoustic 100mm

Aggregate Industries UK Ltd, North End, Ashton Keynes, Wiltshire - Tel: 01285 646900 - Fax: 01285 646949

- Website: www.aggregate.com/concrete-blocks

Project Title:

# Masonry Specifications

355 Concrete Common Blockwork to (insert location to be painted)

Blocks to BS EN 771 - 3

Manufacturer: Aggregate Industries UK Ltd, Croft Works, Marions way, Croft, Leicestershire, LE9 3GP, Tel 01455 285670

Product reference: Masterlite Pro Acoustic Paintgrade

Configuration: Solid (Group 1)

Compressive Strength:

Minimum mean: 7.3 N/mm2

Characteristic: N/A

Category: II

Freeze/Thaw resistance: Frost Resistant

Recycled Content: N/A

Work size: 440 x 100 x 215

Finish/Colour: Standard

Special Shapes: See Drawings

Additional requirements:

Average density: 1450 kg/m3

Thermal Resistance: 0.175 m2 K/W @ 3 % m/c

Sound Insulation: 45 RwdB (when painted)

Fire Resistance (load bearing): 2 Hrs (Single leaf, No finishes)

Mortar: As Section Z21

Standard: BS EN 998 - 2

Mix: (1:1:6)

Mortar Colour: Natural

Bond: Half bond Stretcher

Joint profile: Bucket Handle

Responsible sourcing level: Excellent

F10 Clause 355 Masterlite Pro Acoustic 140mm

Aggregate Industries UK Ltd, North End, Ashton Keynes, Wiltshire - Tel: 01285 646900 - Fax: 01285 646949

- Website: www.aggregate.com/concrete-blocks

Project Title:

# Masonry Specifications

355 Concrete Common Blockwork to (insert location to be painted)

Blocks to BS EN 771 - 3

Manufacturer: Aggregate Industries UK Ltd, Croft Works, Marions way, Croft, Leicestershire, LE9 3GP, Tel 01455 285670

Product reference: Masterlite Pro Acoustic Paintgrade

Configuration: Solid (Group 1)

Compressive Strength:

Minimum mean: 7.3 N/mm2

Characteristic: N/A

Category: II

Freeze/Thaw resistance: Frost Resistant

Recycled Content: N/A

Work size: 440 x 140 x 215

Finish/Colour: Standard

Special Shapes: See Drawings

Additional requirements:

Average density: 1450 kg/m3

Thermal Resistance: 0.246 m2 K/W @ 3 % m/c

Sound Insulation: 50 RwdB (when painted)

Fire Resistance (load bearing): 2 Hrs (Single leaf, No finishes)

Mortar: As Section Z21

Standard: BS EN 998 - 2

Mix: (1:1:6)

Mortar Colour: Natural

Bond: Half bond Stretcher

Joint profile:  Bucket Handle

Responsible sourcing level: Excellent