F10 Clause 255 Masterblock – Masterlite Pro Fairfaced

Aggregate Industries UK Ltd, North End, Ashton Keynes, Wiltshire - Tel: 01285 646900 - Fax: 01285 646949

- Website: www.aggregate.com/concrete-blocks

Please press CTRL and click on a product below to go to the Specification (all below)

Solid 100mm Grey Fairfaced – inner leaf

Solid 100mm Standard Fairfaced – outer leaf

Solid 140mm Grey Fairfaced – inner leaf

Solid 140mm Standard Fairfaced – outer leaf

F10 Clause 255 Masterblock Masterlite Pro Solid 100mm Fairfaced Internal Grey

Aggregate Industries UK Ltd, Ashton Keynes, Wiltshire - Tel: 01285 646900 - Fax: 01285 646949

- Website: www.aggregate.com/concrete-blocks

Project Title:

# Masonry Specifications

255 Concrete Facing Blockwork to Internal leaf of insulated internal cavity wall

Blocks to BS EN 771 - 3

Manufacturer: Aggregate Industries UK Ltd, North End, Ashton Keynes, Wiltshire, SN6 6QX, Tel 01285 646900

Product reference: Masterlite Pro Fairfaced

Configuration: Solid (Group 1)

Compressive Strength:

Minimum mean: 10.4 N/mm2

Characteristic: N/A

Category: II

Freeze/Thaw resistance: Frost Resistant

Recycled Content: N/A

Work size: 440 x 100 x 215

Finish/Colour: Fairfaced / Grey

Special Shapes: See Drawings

Additional requirements:

Average density: 1450 kg/m3

Thermal Resistance: 0.175 m2 K/W @ 3 % m/c

Sound Insulation: 39 RwdB

Fire Resistance (load bearing): 2 Hrs (Single leaf, no finishes)

Mortar: As Section Z21

Standard: BS EN 998 - 2

Mix: (1:1:6)

Mortar Colour: Natural

Bond: Half bond Stretcher

Joint profile: Bucket Handle

Responsible Sourcing level: Excellent

F10 Clause 255 Masterblock Masterlite Pro Solid 100mm Fairfaced External Standard

Aggregate Industries UK Ltd, North End, Ashton Keynes, Wiltshire - Tel: 01285 646900 - Fax: 01285 646949

- Website: www.aggregate.com/concrete-blocks

Project Title:

# Masonry Specifications

255 Concrete Facing Blockwork to External leaf to insulated external cavity wall

Blocks to BS EN 771 - 3

Manufacturer: Aggregate Industries UK Ltd, North End, Ashton Keynes, Wiltshire, SN6 6QX, Tel 01285 646900

Product reference: Masterlite Pro Fairfaced

Configuration: Solid (Group 1)

Compressive Strength:

Minimum mean: 10.4 N/mm2

Characteristic: N/A

Category: II

Freeze/Thaw resistance: Frost Resistant

Recycled Content: N/A

Work size: 440 x 100 x 215

Finish/Colour: Standard

Special Shapes: See Drawings

Additional requirements:

Average density: 1450 kg/m3

Thermal Resistance: 0.164 m2 K/W @ 5 % m/c

Sound Insulation: 39 RwdB

Fire Resistance (load bearing): 2 Hrs (single leaf, no finishes)

Mortar: As Section Z21

Standard: BS EN 998 - 2

Mix: (1:1:6)

Mortar Colour: Natural

Bond: Half bond Stretcher

Joint profile: Bucket Handle

Responsible Sourcing level: Excellent

F10 Clause 255 Masterblock Masterlite Pro Solid 140mm Fairfaced Internal Grey

Aggregate Industries UK Ltd, Ashton Keynes, Wiltshire - Tel: 01285 646900 - Fax: 01285 646949

- Website: www.aggregate.com/concrete-blocks

Project Title:

# Masonry Specifications

255 Concrete Facing Blockwork to Internal leaf of insulated internal cavity wall

Blocks to BS EN 771 - 3

Manufacturer: Aggregate Industries UK Ltd, North End, Ashton Keynes, Wiltshire, SN6 6QX, Tel 01285 646900

Product reference: Masterlite Pro Fairfaced

Configuration: Solid (Group 1)

Compressive Strength:

Minimum mean: 10.4 N/mm2

Characteristic: N/A

Category: II

Freeze/Thaw resistance: Frost Resistant

Recycled Content: N/A

Work size: 440 x 140 x 215

Finish/Colour: Fairfaced / Grey

Special Shapes: See Drawings

Additional requirements:

Average density: 1450 kg/m3

Thermal Resistance: 0.246 m2 K/W @ 3 % m/c

Sound Insulation: 41 RwdB

Fire Resistance (load bearing): 2 Hrs (single leaf, no finishes)

Mortar: As Section Z21

Standard: BS EN 998 - 2

Mix: (1:1:6)

Mortar Colour: Natural

Bond: Half bond Stretcher

Joint profile: Bucket Handle

Responsible Sourcing level: Excellent

F10 Clause 255 Masterblock Masterlite Pro Solid 140mm Fairfaced External Standard

Aggregate Industries UK Ltd, Ashton Keynes, Wiltshire - Tel: 01285 646900 - Fax: 01285 646949

- Website: www.aggregate.com/concrete-blocks

Project Title:

# Masonry Specifications

255 Concrete Facing Blockwork to External leaf of insulated external cavity wall

Blocks to BS EN 771 - 3

Manufacturer: Aggregate Industries UK Ltd, North End, Ashton Keynes, Wiltshire, SN6 6QX, Tel 01285 646900

Product reference: Masterlite Pro Fairfaced

Configuration: Solid (Group 1)

Compressive Strength:

Minimum mean: 10.4 N/mm2

Characteristic: N/A

Category: II

Freeze/Thaw resistance: Frost Resistant

Recycled Content: N/A

Work size: 440 x 140 x 215

Finish/Colour: Standard

Special Shapes: See Drawings

Additional requirements:

Average density: 1450 kg/m3

Thermal Resistance: 0.230 m2 K/W @ 5 % m/c

Sound Insulation: 41 RwdB

Fire Resistance (load bearing): 2 Hrs (single leaf, no finishes)

Mortar: As Section Z21

Standard: BS EN 998 - 2

Mix: (1:1:6)

Mortar Colour: Natural

Bond: Half bond Stretcher

Joint profile: Bucket Handle

Responsible Sourcing level: Excellent