F10 Clause 355 Masterblock – Masterlite Pro

Aggregate Industries UK Ltd, North End, Ashton Keynes, Wiltshire - Tel: 01285 646900 - Fax: 01285 646949

- Website: www.aggregate.com/concrete-blocks

Please press CTRL and click on a product below to go to the Specification (all below)

Masterlite Pro Standard Solid 100mm

Masterlite Pro Standard Solid 100mm - External

Masterlite Pro Standard Solid 100mm - Paintgrade

Masterlite Pro Standard Solid 140mm

Masterlite Pro Standard Solid 140mm - Paintgrade

F10 Clause 355 – Masterlite Pro Standard Solid 100mm

Aggregate Industries UK Ltd, North End, Ashton Keynes, Wiltshire - Tel: 01285 646900 - Fax: 01285 646949

- Website: www.aggregate.com/concrete-blocks

Project Title:

# Masonry Specifications

355 Concrete Common Blockwork to (insert location & finish to be applied)

Blocks to BS EN 771 - 3

Manufacturer: Aggregate Industries UK Ltd, North End, Ashton Keynes, Wiltshire, SN6 6QX, Tel 01285 646900

Product reference: Masterlite Pro Standard

Configuration: Solid (Group 1)

Compressive Strength:

Minimum mean: 7.3 N/mm2

Characteristic: N/A

Category: II

Freeze/Thaw resistance: Frost Resistant

Recycled Content: N/A

Work size: 440 x 100 x 215

Finish/Colour: Standard

Special Shapes: See Drawings

Additional requirements:

Average density: 1450 kg/m3

Thermal Resistance: 0.175 m2 K/W @ 3 % m/c

Sound Insulation: 42 RwdB

Fire Resistance (load bearing): 2 Hrs (Single leaf, No finishes)

Mortar: As Section Z21

Standard: BS EN 998 - 2

Mix: (1:1:6)

Mortar Colour: Natural

Bond: Half bond Stretcher

Joint profile: Bucket Handle

Responsible sourcing level: Excellent

F10 Clause 355 - Masterlite Pro Standard 100mm - External

Aggregate Industries UK Ltd, North End, Ashton Keynes, Wiltshire - Tel: 01285 646900 - Fax: 01285 646949

- Website: www.aggregate.com/concrete-blocks

Project Title:

# Masonry Specifications

355 Concrete Common Blockwork to External leaf to insulated external cavity wall, to receive render

Blocks to BS EN 771 - 3

Manufacturer: Aggregate Industries UK Ltd, North End, Ashton Keynes, Wiltshire, SN6 6QX, Tel 01285 646900

Product reference: Masterlite Pro Standard

Configuration: Solid (Group 1)

Compressive Strength:

Minimum mean: 7.3 N/mm2

Characteristic: N/A

Category: II

Freeze/Thaw resistance: Frost Resistant

Recycled Content: N/A

Work size: 440 x 100 x 215

Finish/Colour: Standard

Special Shapes: See Drawings

Additional requirements:

Average density: 1450 kg/m3

Thermal Resistance: 0.164 m2 K/W @ 5 % m/c

Sound Insulation: 42 RwdB

Fire Resistance (load bearing): 2 Hrs (Single leaf, No finishes)

Mortar: As Section Z21

Standard: BS EN 998 - 2

Mix: (1:1:6)

Mortar Colour: Natural

Bond: Half bond Stretcher

Joint profile: Raked back to receive render

Responsible sourcing level: Excellent

F10 Clause 355 - Masterlite Pro Standard 100mm - Paintgrade

Aggregate Industries UK Ltd, North End, Ashton Keynes, Wiltshire - Tel: 01285 646900 - Fax: 01285 646949

- Website: www.aggregate.com/concrete-blocks

Project Title:

# Masonry Specifications

355 Concrete Common Blockwork to (insert location to receive paint finish)

Blocks to BS EN 771 - 3

Manufacturer: Aggregate Industries UK Ltd, North End, Ashton Keynes, Wiltshire, SN6 6QX, Tel 01285 646900

Product reference: Masterlite Pro Paintgrade

Configuration: Solid (Group 1)

Compressive Strength:

Minimum mean: 7.3 N/mm2

Characteristic: N/A

Category: II

Freeze/Thaw resistance: Frost Resistant

Recycled Content: N/A

Work size: 440 x 100 x 215

Finish/Colour: Paintgrade

Special Shapes: See Drawings

Additional requirements:

Average density: 1450 kg/m3

Thermal Resistance: 0.175 m2 K/W @ 3 % m/c

Sound Insulation: 42 RwdB

Fire Resistance (load bearing): 2 Hrs (Single leaf, No finishes)

Mortar: As Section Z21

Standard: BS EN 998 - 2

Mix: (1:1:6)

Mortar Colour: Natural

Bond: Half bond Stretcher

Joint profile: Bucket Handle

Responsible sourcing level: Excellent

F10 Clause 355 - Masterlite Pro Standard Solid 140mm

Aggregate Industries UK Ltd, North End, Ashton Keynes, Wiltshire - Tel: 01285 646900 - Fax: 01285 646949

- Website: www.aggregate.com/concrete-blocks

Project Title:

# Masonry Specifications

355 Concrete Common Blockwork to (insert location & finish to be applied)

Blocks to BS EN 771 - 3

Manufacturer: Aggregate Industries UK Ltd, North End, Ashton Keynes, Wiltshire, SN6 6QX, Tel 01285 646900

Product reference: Masterlite Pro Standard

Configuration: Solid (Group 1)

Compressive Strength:

Minimum mean: 7.3 N/mm2

Characteristic: N/A

Category: II

Freeze/Thaw resistance: Frost Resistant

Recycled Content: N/A

Work size: 440 x 140 x 215

Finish/Colour: Standard

Special Shapes: See Drawings

Additional requirements:

Average density: 1450 kg/m3

Thermal Resistance: 0.246 m2 K/W @ 3 % m/c

Sound Insulation: 44 RwdB

Fire Resistance (load bearing): 2 Hrs (Single leaf, No finishes)

Mortar: As Section Z21

Standard: BS EN 998 - 2

Mix: (1:1:6)

Mortar Colour: Natural

Bond: Half bond Stretcher

Joint profile: Bucket Handle

Responsible sourcing level: Excellent

F10 Clause 355 Masterlite Pro Standard Solid 140mm - Paintgrade

Aggregate Industries UK Ltd, North End, Ashton Keynes, Wiltshire - Tel: 01285 646900 - Fax: 01285 646949

- Website: www.aggregate.com/concrete-blocks

Project Title:

# Masonry Specifications

355 Concrete Common Blockwork to (insert location to receive paint finish)

Blocks to BS EN 771 - 3

Manufacturer: Aggregate Industries UK Ltd, North End, Ashton Keynes, Wiltshire, SN6 6QX, Tel 01285 646900

Product reference: Masterlite Pro Paintgrade

Configuration: Solid (Group 1)

Compressive Strength:

Minimum mean: 7.3 N/mm2

Characteristic: N/A

Category: II

Freeze/Thaw resistance: Frost Resistant

Recycled Content: N/A

Work size: 440 x 140 x 215

Finish/Colour: Paintgrade

Special Shapes: See Drawings

Additional requirements:

Average density: 1450 kg/m3

Thermal Resistance: 0.246 m2 K/W @ 3 % m/c

Sound Insulation: 44 RwdB

Fire Resistance (load bearing): 2 Hrs (Single leaf, No finishes)

Mortar: As Section Z21

Standard: BS EN 998 - 2

Mix: (1:1:6)

Mortar Colour: Natural

Bond: Half bond Stretcher

Joint profile: Bucket Handle

Responsible sourcing level: Excellent